## Slide 1
BATTERY THERMAL MODELLING
Goal: Build a Predictive
Thermal Model for Zn-MnO₂ Cells
Calibrate and validate a model that predicts cell temperature
during charge/discharge — using only directly measured parameters.
What the model gives you
Predict T(t)
Temperature over time during any duty cycle
Validate safely
Confirm cell stays within thermal limits
Tune cooling
Design the optimal enclosure & airflow
Age accurately
Track R0 growth to predict end-of-life
m·c_p · dT/dt = I²·R0 − h·A·(T − T_amb)
Governing equation: lumped thermal model
Weekly Progress Update | April 2026

## Slide 2
Experiment Plan
Four sequential tests — three parameters measured directly from data
1
h_conv Measurement
Method
44 A pulse → OCV cool-down
Output
Fit T(t) = T∞ + ΔT·e^(−t/τ)
Completed ✓
2
R0 Measurement (GITT)
Method
22 A / 10 s pulses, 100% → 10% SOC
Output
R0 = |ΔV| / I at each SOC
Completed ✓
3
Calibration Cycling
Method
15 A & 30 A, 30 min pulses, 200 h
Output
Validate model + ageing rate
Next step ⟶
4
Validation Test
Method
Unseen current level on fresh cell
Output
Blind prediction vs. measurement
Future
Parameters: h_conv — measured from Test 1 | R0 — measured from Test 2 | k_radial — from datasheet | Ageing rate — verified in Test 3

## Slide 3
Test 1: Convection Coefficient (h_conv)
44 A pulse → full OCV cool-down | Fitted: T(t) = T∞ + ΔT₀ · exp(−t/τ) | h = m·c_p / (τ·A)
1.46
W/m²·K
h_conv RT (23°C)
2.44
W/m²·K
h_conv 40°C
τ = 676 min
RT time constant
Physical Parameters
m = 3 kg (jelly roll mass)
c_p = 1400 J/kg·K
A = 0.0709 m² (outer surface)
Fit Quality (R²)
RT: 0.931 ← good
40°C: 0.839 (ΔT only 1°C)
Method
Q_gen = 0 during OCV rest
Fit ln(T − T∞) vs time
Slope = −1/τ
h = m·c_p / (τ · A)
Chart: RT Cool-down Curve
| 0 | 0.08 | 0.16 | 0.25 | 0.33 | 0.42 | 0.5 | 0.58 | 0.67 | 0.75 | 0.83 | 0.92 | 1 | 1.08 | 1.17 | 1.25 | 1.33 | 1.42 | 1.5 | 1.58 | 1.67 | 1.75 | 1.83 | 1.92 | 2 | 2.17 | 2.33 | 2.5 | 2.67 | 2.83 | 3 | 3.25 | 3.5 | 3.75 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12
Measured T_center (°C) | 30.87 | 30.86 | 30.8 | 30.74 | 30.67 | 30.58 | 30.58 | 30.54 | 30.48 | 30.36 | 30.28 | 30.23 | 30.12 | 30.04 | 29.95 | 29.86 | 29.8 | 29.64 | 29.62 | 29.55 | 29.27 | 29.14 | 28.99 | 28.91 | 28.83 | 28.64 | 28.41 | 28.28 | 27.98 | 27.87 | 27.82 | 27.71 | 27.57 | 27.58 | 27.52 | 27.12 | 26.96 | 26.5 | 26.56 | 26.57 | 26.62 | 26.22 | 26.08 | 25.97 | 25.94 | 25.91 | 25.72 | 25.63 | 25.66 | 25.5 | 25.72
Exponential fit | 30.87 | 30.814 | 30.759 | 30.697 | 30.643 | 30.582 | 30.528 | 30.475 | 30.416 | 30.363 | 30.311 | 30.253 | 30.201 | 30.151 | 30.094 | 30.043 | 29.994 | 29.938 | 29.889 | 29.84 | 29.786 | 29.738 | 29.69 | 29.637 | 29.59 | 29.491 | 29.4 | 29.304 | 29.209 | 29.122 | 29.03 | 28.898 | 28.768 | 28.642 | 28.518 | 28.278 | 28.049 | 27.83 | 27.62 | 27.42 | 27.228 | 27.044 | 26.869 | 26.701 | 26.54 | 26.386 | 26.239 | 26.099 | 25.964 | 25.835 | 25.712
⚠ 40°C note: ΔT above ambient was only 1°C, giving a noisier fit (R² = 0.84). Consider repeating with a larger heating pulse to improve confidence in the 40°C h_conv value.

## Slide 4
Test 2: Internal Resistance R0 — GITT
22 A × 10 s pulses at 10% SOC steps | R0 = |ΔV| / I | Mid-SOC average used as model value
2.03 mΩ
mid-SOC avg
R0 RT (23°C)
1.97 mΩ
mid-SOC avg
R0 40°C
−3%
lower R at higher T ✓
Ratio 40°C / RT
Chart: R0 vs SOC — Both Conditions
| 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30 | 20 | 10
RT (23°C) | 2.75 | 3.27 | 2.31 | 2.05 | 1.25 | 1.24 | 2.95 | 2.05 | 2.35 | 2.87
40°C | 3.15 | 2.7 | 2.4 | 2.37 | 2.08 | 2.42 | 2 | 1.28 | 1.23 | 2.94
Data Quality
100%
Caution
90%
Caution
80%
Acceptable
70%
Acceptable
60%
Caution
50%
Good
40%
Caution
30%
Acceptable
20%
Caution
10%
Good
Model R0 value: mid-SOC average (20–80% SOC) where response is flat and measurement is most reliable
RT: 2.028 mΩ (0.002028 Ω) | 40°C: 1.967 mΩ (0.001967 Ω) | Data quality flags: Good ≤30 s lag · Acceptable ≤120 s · Caution >120 s

## Slide 5
NEXT STEPS
Calibration Cycling — Set Up 22 A & 44 A Tests
01
Set up 22 A & 44 A cycling tests
Load protocols onto PEC machines. Run both cells simultaneously in the same temperature-controlled chamber at 25°C to ensure identical ambient for both.
This week
02
Pre-condition & start 200 h loop
Discharge each cell to 50% SOC before starting. Confirm voltage cutoffs (1.00 V / 1.85 V) are set as hard channel limits. Start both channels at the same time.
This week
03
Monitor & begin model implementation
Check first 24 h for SOC drift or unexpected cutoff triggers. Begin coding the thermal model in parallel using the h_conv and R0 values already measured.
Next week
h_conv: 1.46 / 2.44 W/m²·K
R0: 2.03 / 1.97 mΩ
k_radial: 0.16 W/m·K
Ageing rate: TBC from Test 3