## Slide 1: Goal: Build a Predictive Thermal Model for Zn-MnO2 Cells
Calibrate and validate a model that predicts cell temperature when cells are subjected to various currents
Malesa Sammy 04/02/2026

## Slide 2: Experimental Plan
Four sequential tests — two parameters measured directly from data
1
Convection coefficient Measurement
Method
44 A pulse → OCV cool-down
Output
Fit T(t) = T∞ + ΔT·e^(−t/τ)
Completed ✓
2
R0 Measurement (GITT)
Method
22 A / 10 s pulses, 100% → 10% SOC
Output
R0 = |ΔV| / I at each SOC
Completed ✓
3
Calibration Cycling
Method
15 A & 30 A, 30 min pulses
Output
Validate model + ageing rate
Next step ⟶
4
Validation Test
Method
Unseen current level on fresh cell
Output
Blind prediction vs. measurement
Future
Parameters: h_conv — measured from Test 1 | R0 — measured from Test 2 | Cycling/Ageing rate — verified in Test 3
1

## Slide 3: Experimental Set Up
One thermocouple inserted halfway down the center of the jellyroll- this measures the center temperature and the entire jellyroll is assumed to be at this temperature.
One thermocouple halfway along the height of the cell canister- this is used as the surface temperature for the model

## Slide 4: Test 1- Convection coefficient (h)
44 A pulse → full OCV cool-down | Fitted: T(t) = T∞ + ΔT₀ · exp(−t/τ) | h = m·c_p / (τ·A)
1.46
W/m²·K
h_conv RT (23°C)
2.44
W/m²·K
h_conv 40°C
τ = 676 min
RT time constant
m = 3 kg (jelly roll mass)
c_p = 1400 J/kg·K
A = 0.0709 m² (outer surface)
Fit Quality (R²)
RT: 0.931 ← good
40°C: 0.839 (ΔT only 1°C)
Method
Q_gen = 0 during OCV rest
Fit ln(T − T∞) vs time
Slope = −1/τ
h = m·c_p / (τ · A)
Chart: RT Cool-down Curve
| 0 | 0.08 | 0.16 | 0.25 | 0.33 | 0.42 | 0.5 | 0.58 | 0.67 | 0.75 | 0.83 | 0.92 | 1 | 1.08 | 1.17 | 1.25 | 1.33 | 1.42 | 1.5 | 1.58 | 1.67 | 1.75 | 1.83 | 1.92 | 2 | 2.17 | 2.33 | 2.5 | 2.67 | 2.83 | 3 | 3.25 | 3.5 | 3.75 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10 | 10.5 | 11 | 11.5 | 12
Measured T_center (°C) | 30.87 | 30.86 | 30.8 | 30.74 | 30.67 | 30.58 | 30.58 | 30.54 | 30.48 | 30.36 | 30.28 | 30.23 | 30.12 | 30.04 | 29.95 | 29.86 | 29.8 | 29.64 | 29.62 | 29.55 | 29.27 | 29.14 | 28.99 | 28.91 | 28.83 | 28.64 | 28.41 | 28.28 | 27.98 | 27.87 | 27.82 | 27.71 | 27.57 | 27.58 | 27.52 | 27.12 | 26.96 | 26.5 | 26.56 | 26.57 | 26.62 | 26.22 | 26.08 | 25.97 | 25.94 | 25.91 | 25.72 | 25.63 | 25.66 | 25.5 | 25.72
Exponential fit | 30.87 | 30.814 | 30.759 | 30.697 | 30.643 | 30.582 | 30.528 | 30.475 | 30.416 | 30.363 | 30.311 | 30.253 | 30.201 | 30.151 | 30.094 | 30.043 | 29.994 | 29.938 | 29.889 | 29.84 | 29.786 | 29.738 | 29.69 | 29.637 | 29.59 | 29.491 | 29.4 | 29.304 | 29.209 | 29.122 | 29.03 | 28.898 | 28.768 | 28.642 | 28.518 | 28.278 | 28.049 | 27.83 | 27.62 | 27.42 | 27.228 | 27.044 | 26.869 | 26.701 | 26.54 | 26.386 | 26.239 | 26.099 | 25.964 | 25.835 | 25.712

## Slide 5: Test 2- Internal Resistance R0
22 A × 10 s pulses at 10% SOC steps | R0 = |ΔV| / I | Mid-SOC average used as model value
2.03 mΩ
mid-SOC avg
R0 RT (23°C)
1.97 mΩ
mid-SOC avg
R0 40°C
−3%
lower R at higher T ✓
Ratio 40°C / RT
Chart: R0 vs SOC — Both Conditions
| 100 | 90 | 80 | 70 | 60 | 50 | 40 | 30 | 20 | 10
RT (23°C) | 2.75 | 3.27 | 2.31 | 2.05 | 1.25 | 1.24 | 2.95 | 2.05 | 2.35 | 2.87
40°C | 3.15 | 2.7 | 2.4 | 2.37 | 2.08 | 2.42 | 2 | 1.28 | 1.23 | 2.94
Model R0 value: mid-SOC average (20–80% SOC) where response is flat and measurement is most reliable
RT: 2.028 mΩ (0.002028 Ω) | 40°C: 1.967 mΩ (0.001967 Ω) | Data quality flags: Good ≤30 s lag · Acceptable ≤120 s · Caution >120 s

## Slide 6: Thermal Model Concept

## Slide 7: Thermal Model Concept
The cell is simplified into a 2-node thermal system:
Core (electrochemical region) → heat generation + storage
Surface (cell can) → heat dissipation to ambient
Heat flows in a 1D thermal path:
Core → Surface → Ambient

## Slide 8: Test 3- Calibration Cycling

## Slide 9: Test 3- Calibration Cycling- Model
Here, the model uses the surface temperature as the ambient condition
Next step: constant ambient temperature

## Slide 10: Test 3- Calibration Cycling- Constant Ambient T

## Slide 11: Test 3- Calibration Cycling- Constant Ambient T
Next Steps:
Determine why the model breaks for the surface temperatures (it gives nan C)
Continue calibrating the model so that the RMSE is </= 1°C
Try the model on other cells